BD-LS (Loop Shield)
Available in GRAY or Black
30floz Tubes
12 Tubes per Case
BD Loop Shield is a tough, long lasting, flexible one-part moisture curing self-leveling hybrid sealant. BD-LS protects and shields inductance loop wire in concrete, asphalt, and other substrates.
BD Loop Shield is 100% solids and will not “shrink” or “dip” after application, providing an even/flat finished loop and seal. BD-LS can be applied to damp or dry surfaces and provides a superior seal while still allowing movement and elongation should the joint contract or expand.
To get the most from your tube of Loop Shield, use with BD Loops Preformed 3/16” Saw-Cut Loops and a 3/16” Saw Blade. Save Time, Money, and Sealant with BD Loops!
Features at a Glance:
	· VOC Compliant
· Fast Skin & Cure time
· Use in All Climates
· Apply to Wet / Damp Substrates
· Tolerates Water Before Curing
· 100% Solids will not Shrink
· Resisting Yellowing
	· Proposition 65 Compliant
· Paintable
· Available in Black & Gray
· Excellent UV Resistance
· Wide Adhesion Range
· Long-Term Durability
· Made in USA


Curing: BD-LS will skin over in approximately 45 minutes at 70°F (21°C) and 50% relative humidity. Temperatures below 32°F (0°C) and/or low humidity will slow the skin/cure time. Strength will start to develop immediately and continue increasing for 7 days after application. However, if groove is slightly underfilled traffic is permitted immediately after application.

Spills/Clean Up: Wet BD-LS can be cleaned with alcohol. Dry BD-LS can be removed by abrading or scraping.
Coverage Per Tube/Case
See chart below.

	3/16” Wide Blade
	¼” Wide Blade

	Depth
	Coverage per Cartridge
	Coverage per Case
	Depth
	Coverage per Cartridge
	Coverage per Case

	1 ¼”
	20ft
	240ft
	1 ¼”
	15ft
	180ft

	1 ½”
	16ft
	192ft
	1 ½”
	12ft
	144ft


It’s better to purchase 1 extra tube of BD-LS than to run out of loop sealant on a jobsite.
Using a 3/16" wide blade over 1/4" blade will save you 25% in loop sealant.
DIRECTIONS
BD Loop Shield is ready to use and requires no mixing or additives. Before sealant application remove dust, debris, and standing water. Suggested ambient temperature range for sealant application: 32°F – 120°F (0°C -48°C).

Application: Carefully cut the tip off the cartridge just above the nozzle threads. Thread sealant tip onto cartridge and place into quart sized caulking gun. Sealant should be applied from the bottom of the saw-cut groove. Slightly underfill the groove to be within 1/8” (3.12 mm) of the surface to prevent vehicles from tracking sealant. For easier application, pneumatic and battery powered dispensing guns are available.
Spills/Clean Up: Wet BD-LS can be cleaned with alcohol. Dry BD-LS can be removed by abrading or scraping.
Storage: For Maximum shelf life store in a dry, cool, and well-ventilated place. 

